Item #216012a - CONTROLLED LOW STRENGTH MATERIAL

Description:  Controlled Low Strength Material (CLSM) is a self consolidating, rigid setting material to be used in backfills, fills, structural fills and elsewhere as indicated on the plans, or as directed by the Engineer.  The flow and set time characteristics of CLSM shall be designed to meet the specific job conditions.  All CLSM material covered by this specification shall be designed to be hand excavatable at any time after placement.  It shall be composed of a mixture of portland cement, aggregate, and water with the option of using fly ash, slag cement, air-entraining agents, and other approved admixtures.

Materials:  All materials utilized in the CLSM mix design shall be in accordance with the applicable requirements of Article M.03.01

Composition:  The composition of the CLSM shall be in accordance with the requirements set forth in Article M.03.01-General Composition of Concrete Mixes, as well as the applicable sections of ACI 229R.  The Contractor shall submit each proposed mix design, with all supporting data, to the Engineer for review and approval at least two weeks prior to its use.

The setting time of CLSM materials shall be designed so as to achieve the strength necessary to comply with the time constraints called for under the Maintenance and Protection of Traffic requirements of the project specifications.  The use of chloride accelerators is not permitted.

The minimum compressive strength of the CLSM material shall be 30 pounds per square inch (psi) and the maximum compressive strength of the CLSM shall be 150 pounds per square inch (psi) when tested in accordance with ASTM D4832 after 56 days.

The CLSM mix design shall utilize a nominal maximum size of No. 8 aggregate as specified in M.01.01.

CLSM mixes shall have a minimum of 20% entrained air when tested in accordance with AASHTO T152.

Construction Methods:  CLSM shall only be placed when the ambient temperature is at least 32° F and rising.   CLSM material shall be deposited within 2 hours of initial mixing.

CLSM may be placed by chutes, conveyors, buckets or pumps depending upon the application and accessibility of the site.  Should voids or cavities remain after the placement of the CLSM, the Contractor shall modify the placement method or flow characteristics of the CLSM.  Voids or cavities which have not been filled properly shall be corrected as directed by the Engineer and at the Contractor's expense.

Method of Measurement:  This work will be measured for payment by the actual number of cubic yards of "Controlled Low Strength Material installed and accepted within the pay limits shown on the contract plans or as directed by the Engineer.

Basis of Payment:  This work will be paid at the contract unit price per cubic yard “Controlled Low Strength Material,” which price shall include all materials, equipment, tools and labor incidental thereto.